ALCHEMY LAB: THE GOLDEN DREAM

***Teacher note:  Because most classrooms do not have enough fume hoods for all students to perform the lab, I generally have students bring in pennies and line up by the fume hood.  I heat the pennies (a couple at a time) in the NaOH and zinc mixture for them.  When the pennies look “silver”, I take them out and drop them in a beaker of water and give the beaker to the student.  The student then takes the penny to the lab station and completes the rest of the procedure.

INTRODUCTION: METALS AND ALLOYS IN OUR LIVES 
Metallic elements silver (Ag), gold (Au) and copper (Cu) are lustrous, malleable, ductile and conductive. For millennia, each has been used to make sculptures, jewelry and structures large and small. Artists often work with alloys like bronze, steel or brass because of their durability and color. Bronze is a mixture of copper and tin; brass, made in the activity below, is a mixture of zinc and copper. Steel is made of iron and carbon. Alloys are used to make coins, jewelry, sculptures and other items.  Alchemists in the Middle Ages believed they could turn ordinary metals into gold. In this lab, you become a 20th-century alchemist and turn pennies into shiny "silver" and "gold".

OBJECTIVE: To observe how an alloy is made.

MATERIALS

3 M NaOH 	                	0.1 g zinc dust 			beaker		hot plate

tongs 				200 mL beaker of water		penny 		Bunsen burner

Safety

NaOH should be handled with great care. It is corrosive and can burn skin. Zinc dust should not be inhaled. Safety goggles should be worn the entire time. Perform in a fume hood.
PROCEDURE

|  | Place half a spoonful of zinc dust in one of your beakers. Add 50 mL of NaOH solution to the dish, on top of the zinc. Set hot plate to medium heat (5) and place the beaker on top. If you are working with a hot plate that has no dial- you must immediately pull out the plug once your liquid starts to bubble even if the 5 minutes is not up! Heat for 5 minutes. Do not boil! When dish is hot, place a penny in it. Heat for two minutes or until the penny is coated and becomes silver in appearance. |
| --- | --- |
|  | Remove the penny from the dish with tongs and drop into water. Gently wipe to remove excess water. |
|  | 6. Using tongs, hold the penny in the flame of a Bunsen burner and gently heat. The penny should turn "gold" (brass). (Do not overheat the penny.) |
|  | 7. Dip the penny in the beaker of water and cool to touch. Be prepared for a sizzle sound. If time permits, you may make more pennies. When completely done, put the NaOH solution in the waste beaker. |